INTERNAL LACQUER FORAMMONIA				370.809

1

Characteristics

HighSolidsinteriorlacquerforcollapsiblealuminiumtubes’protection.Theexclusiveformulation,basedonahighmolecularweightepoxyphenolicresinandfullyetherifiedaminoresincombinationbeingcross-linkedviaaninnovativehardener,yieldsafilmshowinganextremelyhighresistancetomanyproducts,especiallyinthealkalinerange.

Thisproductisabletopasswarmammoniaresistancetestsinsometypicaltestingconditions.

Thehighsolidscontentprovidesfilmswhicharefreeofmicro-porosityandsaggingdefectsevenathighthickness.

2

Technical Data

——————————————————————————————————————————

Color:	gold

——————————————————————————————————————————

Gloss:

——————————————————————————————————————————

Supply viscosity:	DIN4at20°C=25”/27”

——————————————————————————————————————————

Solids content:	47,800±2%

——————————————————————————————————————————

Density:	1,010±0,050 gr/cm3

——————————————————————————————————————————

Recommended film thickness:

——————————————————————————————————————————

Theoretical coverage(dry film10µ):	40,400±2m2/Kg

——————————————————————————————————————————

Storage stability(sealedoriginalpackagingat25°C.):	6 months

——————————————————————————————————————————

MOD24 –Rev.01						(Rev.05 March 2015) -page 1

3

Application Instructions

——————————————————————————————————————————

Substrate:	aluminium

——————————————————————————————————————————

Pretreatment:	annealing

——————————————————————————————————————————

Application method:	spray

——————————————————————————————————————————

Recommended coating system:	onecoat

——————————————————————————————————————————

Mixing ratio:

——————————————————————————————————————————

Pot-life:

——————————————————————————————————————————

Thinner:	900084ifnecessary

——————————————————————————————————————————

Application viscosity:	as supplied

——————————————————————————————————————————

Flash-off:

——————————————————————————————————————————

Curing time:	5’at280°-290°C	7’at270°-280°C

——————————————————————————————————————————

4

Remarks

(rev.05 March 2015) -page. 2